# FS5.2  |  Lay-on system with plaster trim profiles

| Pos............................ ..............................m² Pos............................ Pos............................ ..................running m | Delivery and installation of durlum metal panels of the System FS5.2. The metal panels are placed form-fitting and tension-free on a special substructure [see separate position]. Easy demounting without tools is ensured. Tolerances and quality requirements according to TAIM, DIN EN 13964 and durlum Standards. Material: Optionally galvanised steel or aluminium/stainless steel Thickness: According to strength requirements Surface finish: D206-700 white powder coated similar to RAL 9016, optional colour RAL ............... Coating thickness: Approx. 70 µm Perforations: durlum Type RG-L15 [2.5/5.5] Sound absorption: By means of a special durlum acoustic fleece s=approx. 0.73, optionally in black or white Dimensions: Length ............... mm Width ............... mm €/m² Start-up costs depending on format, training and call-up € Delivery and installation of a durlum System FS5.2 substructure consisting of RS 1401 gypsum trim profiles of aluminium which are suspended from the bare ceiling with slideable AH 161 locking holders, nonius lower and upper parts and officially approved dowel plugs. The profiles are to be attached completely horizontal and parallel running to each other. The spacing of the suspension points is according to DIN 18168, DIN EN 13964 and the loads of the system and to be checked by the contractor. It is only permissible to use structure components that have been approved by the manufacturer of the metal panels. All parts are made of galvanised steel or aluminium. €/running m |
| --- | --- |