# FF2025 RHOMBOS  |  Suspension system with shadow gap

| Pos............................ ..............................m² Pos............................ Pos............................ .............................running metre | Delivery and installation of durlum expanded metal panels of the FF2025 RHOMBOS V1 system. A frame is butt welded onto the cut-to-size expanded metal panels. By this, precisely fitting parts are produced which are cut for tolerance compensation and placed with one side onto the edge profiles [see separate position]. The other side of the panels is placed in a positive-locking and tension-free way onto the profiles. Easy and tool-free dismounting is guaranteed. Tolerances and quality requirements apply according to TAIM, DIN EN 13964 and durlum standard. Material: electrolytically galvanised steel Variant: V1 (surface-welded frame) Mesh M260_1.5 Mesh length: 28 mm Mesh width: 12 mm Web width: 2.0 mm Web thickness: 1.5 mm Exp. metal thickness: approx. 3.6 mm Surface: Powder-coated similar to RAL9006-079 smooth and shiny (alternative RAL......) Layer thickness: approx. 60 µm Sound absorption: with a special durlum acoustic fleece and support Colour: black Dimension: Length ............... mm Width ............... mm € / m2 Set-up costs depending on format, design and call-off € Delivery and installation of durlum edge profiles F 2025 made of aluminium. The profiles must be mounted vertically to the corridor wall so that the expanded metal panel can be inserted. The mounted profiles must be perfectly level. Use only officially approved dowels. The distance between the attachment points has to be defined according to DIN EN 13964 and the static load of the system and is to be verified by the contractor. Only constructions may be used that have been approved by the manufacturer of the expanded metal panels. Material thickness: 1.5 mm Surface: Powder-coated similar to RAL9006-079 smooth and shiny (alternative RAL......) Profile form: according to durlum F 2025 with shadow gap 25/20/20/25 mm €/running |
| --- | --- |