# FS5.2 FH RHOMBOS  |  Attachment system with gypsum board end profile

| Pos............................ ..............................m² Pos............................ Pos............................ .............................linear metre | Delivery and installation of durlum expanded metal panels of the FS5.2 FH RHOMBOS V1 system. A frame is butt welded onto the cut-to-size expanded metal panels. In this manner, precisely fitting parts are produced that are suspended in a positive-locking and tension-free way by means of a special substructure [see separate position]. Easy and tool-free dismounting is guaranteed. Tolerances and quality requirements apply according to TAIM, DIN EN 13964 and durlum standard. Material: electrolytically galvanised steel Variant: V1 (surface-welded frame) Mesh M260_1.5 Mesh length: 28 mm Mesh width: 12 mm Web width: 2.0 mm Web thickness: 1.5 mm Exp. metal thickness: approx. 3.6 mm Surface: Powdercoated similar to RAL9006-079 smooth and shiny (alternative RAL......) Layer thickness: approx. 60 µm Sound absorption: with a special durlum acoustic fleece and support Colour: black Dimension: Length ............... mm Width ............... mm € / m2 Set-up costs depending on format, design and call-off € Delivery and installation of a durlum FS5.2 FH substructure consisting of a perimeter trim for gypsum RS 1401 made of aluminium, which is suspended from the bare ceiling via a movable clamping bracket AH 161 using vernier scale upper and lower parts and officially approved dowels. The profiles must be perfectly level and parallel to each other. The distance between the suspension points has to be defined according to DIN EN 13964 and the static load of the system and is to be verified by the contractor. Only constructions may be used that have been approved by the manufacturer of the expanded metal panels. All parts are made of galvanised steel sheet or aluminium. €/running metre |
| --- | --- |