# S1 RHOMBOS | Clip-in system

| Pos............................ ..............................m2 Pos............................ Pos............................ ..............................m2 Pos............................ .............................running metre | Delivery and installation of durlum expanded metal panels of the S1 RHOMBOS system. The long sides of the expanded metal panel are provided with a strengthening bead and are force-fitted into a special substructure [separate position] with the help of clamping cams. The expanded metal panels can be extracted and removed from the clip-in system using a dismounting tool. This guarantees free access to the ceiling void. Tolerances and quality requirements apply according to TAIM, DIN EN 13964 and durlum standard. Material: electrolytically galvanised steel Variant: V5 Mesh M260 Mesh length: 28 mm Mesh width: 12 mm Web width: 2.0 mm Web thickness: 1.0 mm Exp. metal thickness: approx. 3.6 mm Surface: Powder-coated similar to RAL9006-079 smooth and shiny (alternative RAL......) Layer thickness: approx. 60 µm Sound absorption: with a special durlum acoustic fleece and support Colour: black Dimension: Length ............... mm Width ............... mm € / m2 Set-up costs depending on format, design and call-up. € Delivery and installation of an S1 RHOMBOS substructure consisting of Sendzimir galvanised clip-in carriers U 1000 H (primary and secondary profiles) which are suspended as L-shaped constructions via carrier cross connectors U 1001 H. The distance between the primary profiles/clip-in carriers has to be defined according to DIN EN 13964 and the installation manual and must be proven and established by the contractor. The profiles are suspended in a compression-resistant manner using vernier scales. Ensure horizontal and flush alignment during installation. Use only officially approved dowels. The primary profiles are connected to the wall by means of a wall bracket U 1010. The spacing of the secondary profiles is to be adjusted precisely to the spacing of the two clip-in sides of the expanded metal panels. Only constructions may be used that have been approved by the manufacturer of the expanded metal panels. Suspension height: ........... mm. € / m2 Delivery and installation of durlum wall connection profiles made of aluminium. Material thickness: 1.5 mm Surface: Powder-coated similar to RAL9006-079 smooth and shiny (alternative RAL......) Profile form: according to durlum perimeter trim without shadow gap 25/25 mm or according to durlum stepped perimeter trim 25/20/20/25 mm € / running metre |
| --- | --- |