# S5.1 RHOMBOS  |  Crosswise C-channel system

| Pos............................ ..............................m2 Pos............................ Pos............................ ..............................m2 Pos............................ ............................. running metre | Delivery and installation of durlum expanded metal panels of the S5.1 RHOMBOS V1 system. Width of the C-channel: 100-150 mm. Module: ............... A frame is butt welded onto the cut-to-size expanded metal panels. By this, precisely fitting parts are produced that are placed in a positive-locking and tension-free way onto a special substructure [see separate position]. Tool-free dismounting is guaranteed. Tolerances and quality requirements apply according to TAIM, DIN EN 13964 and durlum standard. Material: electrolytically galvanised steel Variant: V1 (surface-welded frame) Mesh M260_1.5 Mesh length: 28 mm Mesh width: 12 mm Web width: 2.0 mm Web thickness: 1.5 mm Exp. metal thickness: approx. 3.6 mm Surface: Powder-coated similar to RAL9006-079 smooth and shiny (alternative RAL......) Layer thickness: approx. 60 µm Sound absorption: with a special durlum acoustic fleece and support Colour: black Dimension: Length ............... mm Width ............... mm € / m2 Set-up costs depending on format, design and call-up. € Delivery and installation of a durlum S5.1 substructure consisting of an L-shaped primary carrier U 1040 as cross-bracing (primary profile) which is suspended from the bare ceiling with the help of vernier scale upper and lower parts or with threaded rods using officially approved dowels in order to ensure a rigid suspension. Suspension height: ........... mm. Width of the C-channel: .... mm. Module: ....... The primary profiles must be connected [screwed] to one another using longitudinal connectors U 1041 at the longitudinal joint. The distance between the primary profiles has to be defined according to DIN EN 13964 and the mounting instructions and must be proven and established by the contractor. The primary profiles are mounted to the walls with wall brackets [U 1042]. C-channels C 2000 are screwed as longitudinal profiles (secondary profiles) to the primary profiles using C-channel hanger brackets C 2007 and screws M6 (secured against loosening). Alternatively, the secondary profiles can be suspended using suspension elements C 2003. Make sure that the structure is swing-free. The longitudinal connection of the secondary profiles is performed using C-channel connectors C 2004. Cross-channels which are precisely cut to length and running transversely to the longitudinal channels at the defined distance are placed on the longitudinal channels via Z-shaped edges. The attachment to the walls is made with wall brackets for C-channels C 2009. The accurately produced expanded metal panels must be inserted between the secondary profiles into the system in order to ensure a tension-free suspension.. Ensure horizontal and flush alignment during installation. Only constructions may be used that have been approved by the manufacturer of the expanded metal panels. All parts are made of galvanised sheet steel. Surface: Powder-coated similar to RAL9006-079 smooth and shiny (alternative RAL......) Layer thickness: approx. 70 µm Material: Galvanised sheet steel or, optionally aluminium or stainless steel €/m2 Delivery and installation of durlum wall connection profiles made of aluminium. Material thickness: 1.5 mm Surface: Powder-coated similar to RAL9006-079 smooth and shiny (alternative RAL......) Profile form: according to durlum F 025 perimeter trim without shadow gap 25/25 mm or according to durlum F 2025 with stepped perimeter trim 25/20/20/25 mm €/running metre |
| --- | --- |