# S1 K  |  Clip-in system, hinged/sliding

| Pos............................ ..............................m² Pos............................ ..............................m² Pos............................ ..................running m | Delivery and installation of durlum metal tiles for system S1 K. The metal tiles are snap-fitted friction-locked into a special substructure using clamping cams. The metal tiles can be extracted from the clip-in system, hinged and pushed together to packets, using a dismounting tool. By slightly twisting them, the metal tiles can also be removed without using tools. Free access to the ceiling void is guaranteed. Tolerances and quality requirements according to TAIM, DIN EN 13964 and durlum Standards. Material: Optionally galvanized sheet steel, aluminium or stainless steel Thickness: Depending on the static requirements Surface finish: Powder-coated with D206-700 white similar to RAL 9016, optional with RAL ............... Coating thickness: Approx. 60µm Perforation: durlum Type RG-L15 [2.5/5.5], 16.20% free cross-section Sound absorption: With a special black durlum acoustic fleece w=approx. 0.73 Dimensions: • Module 600: 600x600mm • Module 625: 625x625mm €/m² Delivery and installation of a durlum system S1 K substructure consisting of U 1000 H sendzimir galvanized clip-in carriers acting as cross bracing [primary profile]. They are suspended from the bare ceiling with nonius suspension elements [rigidly] or quick fixing hangers using officially approved dowels. The primary profiles must be connected to one another at the longitudinal joints using U 1002 longitudinal connectors. The primary profiles are joined to the walls using the wall bracket U 1010. The spacing of the primary profiles depends on the requirements of DIN EN 13964 and the statics of the system and must be proven and established by the contractor. Ensure horizontal and flush alignment during installation. The primary profiles U 1000 H are connected to the secondary profiles U 1000 H using U 1001 H cross connectors. The secondary profiles are connected to one another at the longitudinal joint using connector U 1002. The U 1010 wall bracket is used for joining the secondary profiles to the wall. The spacing of the secondary profiles must be adjusted precisely to 600mm and 625mm, respectively. Ensure horizontal and flush alignment during installation. You have to use constructions, which are approved by the manufacturer of the metal tiles. €/m² Delivery and installation of durlum wall connection profiles. Surface finish: Powder-coated with D206-700 white similar to RAL 9016, optional with RAL ............... Profile: • Perimeter trim F 025 made of aluminium • Perimeter trim F 2025 made of aluminium • Perimeter trim L 020 made of aluminium with fixing clip U 020 • U-profile U 1058 K made of sheet steel with spring clip U 1065 K • Picture-rail trim 031 made of aluminium €/running m |
| --- | --- |