# S5.1-100/150  |  C-channel lateral grid system

| Pos............................ ..............................m2 Pos............................ Pos............................ ..............................m2 Pos............................ ..................running m | Delivery and installation of durlum metal panels of the System S5.1. Band grid width: 100 mm Module: ............... The metal panels are placed form-fitting and tension-free on a special substructure [see separate position]. Demounting is preformed without tools. Tolerances and quality requirements according to TAIM, DIN EN 13964 and durlum Standards. Material: Optionally galvanised steel or aluminium/stainless steel Thickness: According to strength requirements Surface finish: D206-700 white powder coated similar to RAL 9016, optional colour RAL ............... Coating thickness: Approx. 70 µm Perforations: durlum Type RG-L15 [2.5/5.5] Sound absorption: By means of a special durlum acoustic fleece s= approx. 0.73, optionally in black or white Dimensions: Length ............... mm Width ................ mm €/m2 Start-up costs depending on format, training and call-up € Delivery and installation of a System S5.1 substructure consisting of U 1040 form fabricated grid angles as a lateral grid which is suspended pressure-rigid from the bare ceiling with nonius adjustable lower and upper parts or with threaded rods using official approved dowel plugs. Suspension height: ............... mm. Band grid width: 100 mm. Module: ............... The grid angles are to be connected together at the ends by means of U 1041 longitudinal connectors [screw fasteners]. The spacing of the grid angles is according to the requirements of DIN 18168, DIN EN 13964 as well as the loads of the system and to be determined and checked by the contractor. The grid angles are attached to the walls with U 1042 wall brackets. On the grid angles, C 2000 C-channels as longitudinal profiles are attached by means of C 2007 channel profile hangers with M6 bolts [secured against loosening]. As an alternative, the C-channels can be suspended with C 2003 point hangers. Care is to be taken to allow swaying freedom. The longitudinal connection of the C-channels is made with C 2004 channel connectors. At the stated distance [axis pitch], transverse channels, which are cut precisely to length, are laid between the longitudinal channels and supported on them by Z-shaped folded elements. The attachment to the walls is made with C 2009 wall brackets. Between the C-channels, the exactly fabricated metal panels are to be laid tension-free. Care is to be taken to ensure horizontal and flush alignment. It is only permissible to use structure components that have been approved by the manufacturer of the metal panels. All parts are made of galvanised steel. Surface finish: D206-700 white powder coated similar to RAL 9016, optional colour RAL ............... Coating thickness: Approx. 70 µm Material: Galvanised steel, optionally aluminium or stainless steel €/m2 Delivery and installation of durlum wall connection profiles of aluminium. Material thickness: 1.5 mm Surface finish: D206-700 white powder coated similar to RAL 9016, optional colour RAL ............... Profile form: According to durlum F 025 perimeter trim without shadow gap 25/25 mm or durlum F 2025 with stepped perimeter trim 25/20/20/25 mm €/running m |
| --- | --- |